## Slide 1
ART: Automated Redox-Titration with Interdigitated Electrode Arrays for Energy Storage Materials
Zirui Wang
3rd year Ph.D. Student
Department of Materials Science and Engineering University of Illinois, Urbana-Champaign (UIUC)
Advisor: Prof. Joaquín Rodríguez-López
247th ECS Meeting, Montreal, Canada
May 20th, 2025

## Slide 2: Redox Flow Batteries for Grid-Level Energy Storage
Pump
Pump
Source/load
Membrane
Molecules 2015, 20 (11), 20499–20517
ACS Energy Lett. 2022, 7 (10), 3337-3344
Highly scalable, decoupled power and capacity
Limitation: Energy density is limited by the solubility of redox-active species
Redox flow battery (RFB)
Cathode
Tank
Anode
Tank
A
A-
B
B+
e-
e-
Current
Redox targeting flow battery (RTFB)
membrane
Source/Load
Charge/discharge
(Cathode tank)
(Anode tank)
Stores energy in a solid material
  Active species concentration up to 20 M
Redox mediators shuttle charges between the solid and electrode via a mediated electron transfer process known as redox targeting

## Slide 3: The Redox Targeting Process in RTFBs
Sci. Adv. 2015, 1 (10), e1500886
ACS Energy Lett. 2022, 7 (10), 3337-3344
ACS Appl. Mater. Interfaces 2022, 14 (5), 6638–6648
Active redox mediator generation in the cell
Solid material chemically charged/discharged in the tank
Thermodynamic driving force: Nernstian potential difference
Kinetics: Follows the Butler-Volmer model
,
Uncharged (S)
Charged (S+)
Electrode
R
O
-e-
Redox mediator
Solid material
Cell
Tank
R
O
(Flow)
(Flow)
Single mediator redox targeting
R
O
Mediator
oxidizes
solid (S+)
Mediator
reduces
solid (S)
R
O
Potential
Potential
Mediator 1
reduces
solid (S)
O1
R1
Mediator 2
oxidizes
solid (S+)
R2
O2
Dual mediator redox targeting
The redox targeting process
Pros: Simple
Cons: Slow kinetics
Pros: Fast kinetics
Cons: Complex, low voltage efficiency

## Slide 4: Challenges in Studying Redox Targeting
Huge chemical/material space to study
Solid material
Inorganic and organic materials
Redox mediators
Mediators with different
Electrolyte compositions
Charge-balancing ions
Electrolyte concentration
Chemistry A European J 2022, 28 (25), e202200149
ACS Energy Lett. 2022, 7 (10), 3337–3344
Joule 2019, 3 (9), 2255–2267
Figure of merits
Fast redox targeting kinetics
Large capacity for the solid material
Summary
Pros: Offers device-level metrics
Cons: Time-consuming, does not directly offer mechanistic insights about the redox targeting process
Without solid
With solid
Battery cycling experiments
Is there a platform that provides more mechanistic insights?
Notes: For redox targeting to work efficiently, it must be optimized. But doing that has its own challenges.

## Slide 5: Redox-Titration with Scanning Electrochemical Microscopy (SECM)
SECM schematics
Anal. Chem. 2025, 97 (15), 8147–8181
Chem. Rev. 2016, 116 (22), 13234-13278
J. Am. Chem. Soc. 2008, 130 (50), 16985–16995
Langmuir 2017, 33 (37), 9455–9463
(Tip: Ultramicroelectrode)
(Substrate: material of interest)
Steady-state
behavior:
O
R
Mass
Transfer
X
O
O
R
O
R
O
R
Mass
Transfer
Redox titration with SECM
Tip generates active species to titrate the charges in the substrate
A transient current increase can be observed
Can couple with simulations to understand the kinetics
Low throughput, not ideal for studying redox targeting due to the large chemical/material space to explore
Current vs. time response
Is there a platform that improves the throughput of studying mediated electron transfer processes in energy storage materials?

## Slide 6: Interdigitated Electrode Arrays (IDAs)
4 IDAs with different gap widths per chip
Two individually addressable working electrode arrays
Batched, high-yield microfabrication
Gap
width
(in μm)
25 bands per array
Multiplexing circuit to control IDAs
Python library to control commercial electrochemical workstations
https://github.com/jrlLAB/hardpotato
ACS Meas. Sci. Au 2023, 3 (1), 62–72
Anal. Chem. 2023, 95 (11), 4840–4845
Device 2023, 1 (5), 100103–100103
Summary
Automated electrochemical measurements can be performed on IDAs using Python
Large, combinatorial studies can be done
Notes: Emphasize myself did all the microfabrication and device packaging

## Slide 7: Redox-Titration with IDAs
Material of
interest
Array 1
Array 2
Performing a cyclic voltammetry (CV) with array 2 alone generates a normal “duck-shape” CV
Pattern the material of interest on array 1
A transient current increase will be observed on the redox titration CV
Current level returns to the baseline after the material has been fully titrated
Notes: These data are simulated.

## Slide 8: Redox Titration of Polypyrrole, a Model System
Polypyrrole (PPy) is a conjugated polymer
Candidate material for electrochemical supercapacitors and dual-ion batteries
Wang, Z; Pence, M; Rodríguez-López, J. (Manuscript in preparation)
Automated Redox Titration of Polypyrrole, a Conductive Polymer
Motivation
Polypyrrole can store anions from the electrolyte once oxidized
Use automated redox titration to study the charge storage behavior of PPy under different conditions
eScience 2021, 1 (2), 186–193
Phys. Chem. Chem. Phys. 2017, 19 (31), 21165–21173

## Slide 9: Electrodeposition of Polypyrrole (PPy) on IDAs
Chem. Soc. Rev. 2000, 29 (5), 283–293
1. Monomer oxidation
2. Dimerization
3. Stabilization
4. Additional combination-stabilizations
Array 1
ON: Oxidation
Array 2
ON: Reduction
Radical concentration
High
Low
Dual Mode:
Confine radicals on array 1
Large oxidative
current
Small reducing current
Array 2 (Clean)
Array 1 (with PPy)
Optical micrograph after deposition
WE: Pt, RE: Ag/AgCl, CE: graphite. WE 2 potential: 0 V vs. Ag/AgCl.
10 mM pyrrole, 0.1 M TBAPF6 in ACN; scan rate: 500 mV/s
Dual mode electrodeposition CV
Array 1
Array 2
PPy must be selectively patterned on one of the electrode arrays
Use dual-mode to limit the monomeric radicals on one of the arrays

## Slide 10: Experimental Workflow and Response
A “duck-shape” baseline CV is obtained
An oxidizing potential is applied
PPy gets oxidized and incorporates anions from electrolyte
Same CV as the baseline was conducted
A total of 3 cycles:
  First cycle: Redox titration CV
  Following cycles: Post-titration validation
Post-titration CV current returns to the baseline level
1. Baseline CV with array 2
2. PPy charging with array 1
3. Titration and post-titration CVs with array 2
WE: Pt, RE: Ag/AgCl, CE: graphite.
0.2 mM Ru(NH3)63+, 0.1/0.5 M KCl, scan rate: 10/25/50 mV/s
Notes: Ruhex is more reductive than the charged form of Ppy

## Slide 11: Behavior of PPy under Low Ionic Strength (0.1 M KCl)
PPy charging curves at different potentials
Baseline-subtracted titration CVs (10 mV/s scan rate)
(10 mV/s)
(50 mV/s)
* Data shown here were from the IDA with 2 μm gap width
Integrate to calculate the stored charge
Integrate to obtain the titrated charge
Finite-element simulations via COMSOL reveals the role of redox titration kinetics
  Slow kinetics
  Cannot establish full titration within the timescale of the CV measurement
  Less titrated charge at a higher CV scan rate
Stored vs. titrated charge comparison
Simulated behavior (10 mV/s)
Notes: “COMSOL” simulations

## Slide 12: Redox Titration under Elevated Ionic Strength (0.5 M KCl)
(10 mV/s)
(50 mV/s)
Stored vs. titrated charge comparison
* Data shown here were from the IDA with 2 μm gap width, 10 mV/s scan rate
Elevated ionic strength (0.5 M KCl) leads to more charge storage in PPy
The influence of electrolyte concentration on the amount of titrated charge only shows up at low CV scan rate
  Further confirms the slow redox-titration kinetics suggested by simulation

## Slide 13: High-Throughput Nature of Our Platform
PPy charging potential (vs. Ag/AgCl)
0.30 0.35 0.40 0.45 0.50 0.55 0.60
500 automated redox titration within 50 hours (2016 CVs, 504 amperometries)
4 IDA gap widths, 7 polypyrrole charging potentials, 3 CV scan rates, and 2 ionic strengths

## Slide 14: Conclusion
IDA is a useful platform to accelerate studies of mediated electron transfer processes for energy storage materials
Developed a workflow to perform automated redox-titration measurements with IDAs to study the charge storage behavior of polypyrrole
Applied COMSOL simulations understand the kinetics of the redox-titration process
Revealed the effect of ionic strength to the charge storage capacity of polypyrrole
Our workflow drastically improves the throughput of redox titration measurements
Wang, Z; Pence, M; Rodríguez-López, J. (Manuscript in preparation)
Notes: Emphasize that I’m preparing a 1st author paper

## Slide 15: Studying Prussian Blue with IDAs
Prussian Blue (PB)
Fe4[Fe(CN)6]3
Prussian White (PW)
Fe4[Fe(CN)6]3
Fe3+
Fe2+
C
N
Cation
Prussian Blue (PB) and its analogues are promising materials for RTFBs
Optimizing their performances requires screening different redox mediators and electrolyte compositions
Could the optimization process be accelerated with automated electrochemistry on IDAs?
Bare Pt
(Array 2)
PB thin film
(Array 1)
Summary
PB can be electrodeposited on the IDAs
We began with a dual-mediator system to study the performance of PB
Optical micrograph after PB deposition
Dual-mediator system

## Slide 16: Automated Redox Targeting of Prussian Blue
Electrochemistry
Inert gas flow
Solution handling
Automated redox targeting with different cations
Summary
Automated redox-targeting can be performed by coupling IDAs with solution handling hardware.
It is now possible to systematically screen a large chemical space: Redox mediators, electrolyte compositions, other Prussian Blue analogues, etc.
“elab”: A solution handling robot

## Slide 17: Acknowledgements
The JRL lab:
Prof. Joaquín Rodríguez-López
Dr. Michael Pence,
Dr. Oliver Rodríguez, Dr. Abhiroop Mishra
Gavin Hazen, Raghuram Gaddam, and Seth Putnam
All the 3rd years in the JRL lab
All the JRL lab members!
Collaborators:
Pacific Northwest National Laboratory
Dr. Eliot Woods and Dr. Ruozhu Feng
UIUC Cleanroom Research Engineers:
Joseph Maduzia, Dr. Ranveer Singh
Dr. Glennys Mensing
The JRL lab, Fall 2024
This work is funded by the Energy Storage Research Alliance "ESRA" (DE-AC02-06CH11357), an Energy Innovation Hub funded by the U.S. Department of Energy, Office of Science, Basic Energy Sciences.
L08-2765 – May 22nd (Thursday) 8:30 – 9:10 AM 512D, presented by Prof. Joaquín Rodríguez-López

## Slide 18: Thank you! Questions?
Contact:
ziruiw2@illinois.edu
joaquinr@illinois.edu
Learn more about our research!